TECHNICAL DESCRIPTION OF FIBER OPTIC CABLE

- Cable construction

| Cable type | A-D2Y-(6-12)-250-652D/657A1-7212 |  |  |
| --- | --- | --- | --- |
| Cable construction 1. Outer sheath: UV-resistant PЕ 2. Strength element of core: Aramid yarns 3. The first layer of the loose tube: PC 4. The second layer of the loose tube: PBT Optical loose tube: 1,7 mm PBT\PC Tube 5. Intramodule compound: Thixotropic compound 6. Optical Fiber: Single-mode Fiber according to ITU-T G.652.D and G.657.A1 |  |  |  |
| Temperature ranges | Storage and transportation temperature | Installation temperature | Operating temperature |
|  | from -40 to +70 °С | from -10 to +60 °С | from -30 to +70 °С |
| Resistance to water penetration | Water resistant |  |  |
| Relative humidity at +350 C, % | 98 |  |  |
| Outer diameter, mm | 2,0±0,1 |  |  |
| Average weight of 1 km of the cable, kg | 4±5% |  |  |

- Mechanical characteristics

| Calculated tensile strength, not less than, kN Dynamic | 0,1 |
| --- | --- |
| Minimum bending radius | 15D |
| Short-term crush test, kN/cm (N/10cm) | 0,1 (1000) |
| Resistance to axial torsion at angle ±360° on 1 m length cable | Resistant |
| Resistance to bends at angle ± 900 with a radius equal to 15 nominal cable diameters | Resistant |
| Resistance to impact 1 J | Resistant |

- Packaging and marking

| Cable factory length, km | 6 |
| --- | --- |
| Package | Coil ОККО №1 (495х445х495) |
| Tolerance, % | ±3,0 |
| Short lengths (customer approval) | Maximum 5% |
| Marking method | Inkjet printing |
| The accuracy of marking, % | ±0,5 |

- Coloring

| Coloring of fibers in loose tube (According to Customer’s requirements color can be different). |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |
| red | green | blue | yellow | white | slate | brown | violet | aqua | black | orange | pink |

- Product data

| Fiber count | 6 | 12 |
| --- | --- | --- |
| Loose tubes x fibers | 1x6 | 1x12 |

Tensile strength value is for maximum number of fibers design