TECHNICAL DESCRIPTION OF FIBER OPTIC CABLE

- Cable construction

| Cable type | A-D(ZN)2Y-(4-24)-200-652D/657A1-7206 |  |  |
| --- | --- | --- | --- |
| Cable construction 1. Outer sheath: UV-resistant PЕ 2. Strength element of core: aramid yarns 3. The first layer of the loose tube: PC 4. The second layer of the loose tube: PBT Optical loose tube: 2,3 mm PBT\PC Tube 5. Intramodule compound: Thixotropic compound 6. Optical Fiber: 200 mkm Single-mode Fiber according to ITU-T G.652.D and G.657.A1 |  |  |  |
| Temperature ranges | Storage and transportation temperature | Installation temperature | Operating temperature |
|  | from -20 to +70 °С | from -10 to +60 °С | from -20 to +70 °С |
| Resistance to water penetration | Water resistant |  |  |
| Relative humidity at +350 C, % | 98 |  |  |
| Outer diameter, mm | 2,9±0,2 |  |  |
| Average weight of 1 km of the cable, kg | 8±5% |  |  |

- Mechanical characteristics

| Calculated tensile strength, not less than, kN Dynamic | 0,25 |
| --- | --- |
| Minimum bending radius | 15D |
| Short-term crush test, kN/cm (N/10cm) | 0,1 (1000) |
| Resistance to axial torsion at angle ±360° on 1 m length cable | Resistant |
| Resistance to bends at angle ± 900 with a radius equal to 15 nominal cable diameters | Resistant |
| Resistance to impact 2 J | Resistant |

- Packaging and marking

| Cable factory length, km | 6 |
| --- | --- |
| Package | Coil ОККО №2 (605x448x605) |
| Tolerance, % | ±3,0 |
| Short lengths (customer approval) | Maximum 5% |
| Marking method | Inkjet printing |
| The accuracy of marking, % | ±0,5 |

- Coloring

| Coloring of fibers in loose tube (According to Customer’s requirements color can be different). M-fiber with black ring mark. |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |
| red | green | blue | yellow | white | slate | brown | violet | aqua | black | orange | pink |
| 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 |
| red+m | green+m | blue+m | yellow+m | white+m | slate+m | brown+m | violet+m | aqua+m | transparent | orange+m | pink+m |

- Product data

| Fiber count | 4 | 6 | 12 | 24 |
| --- | --- | --- | --- | --- |
| Loose tubes x fibers | 1x4 | 1x6 | 1x12 | 1x24 |

Tensile strength value is for maximum number of fibers design